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SURVEY 713 CES-ENV-27-014
Wall-system asbestos survey
Mother Base Community Support Center · Building 620 · Final signed record
	INSPECTION DATES
	11–13 May 2027

	REPORT DATE
	18 May 2027

	SURVEY SCOPE
	All identified accessible interior and exterior wall-system types

	LABORATORY
	Arctic Analytical Services · Exercise Laboratory AAS-027

	METHOD
	Bulk sampling and polarized-light microscopy; asbestos reported at less than 1 percent as negative


SURVEY RECORD
	SAMPLES
	WALL-SYSTEM AREA
	TESTED
	POSITIVE
	RESULT

	W-01–03
	Administrative-suite gypsum systems
	3
	0
	NEGATIVE

	W-04–06
	Activity and recreation-room systems
	3
	0
	NEGATIVE

	W-07–09
	Multipurpose-hall wall systems
	3
	0
	NEGATIVE

	W-10–12
	Kitchen and dining wall systems
	3
	0
	NEGATIVE

	W-13–15
	Service, storage, and utility systems
	3
	0
	NEGATIVE

	W-16–18
	Perimeter wall finishes and coatings
	3
	0
	NEGATIVE

	TOTAL WALL-SYSTEM SAMPLES
	18
	0
	ALL NEGATIVE


SURVEY CONCLUSION. All wall-system samples tested negative. No asbestos-containing material was identified in the Community Support Center wall systems included in this survey.
LIMITATION. This record addresses wall systems only. It does not clear roofing, flooring, mechanical insulation, equipment, underground materials, or inaccessible non-wall components.
	/s/ NAOMI HUNTER
NAOMI HUNTER, GS-12, DAF
Certified Asbestos Inspector · 713 CES/CEIE
Signed 18 May 2027
	/s/ HAL EMMERICH
HAL EMMERICH, NH-03, DAF
Chief Facilities Engineer · 713 CES/CEN
CES concurrence · 18 May 2027
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