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Campbell Hall interior wall systems | Report SM-PLM-27-114
	Client
	713th Civil Engineer Squadron (713 CES)

	Collected
	7–8 July 2027 by Dr. Para-Medic, CIH

	Analyzed
	9 July 2027 by polarized-light microscopy with dispersion staining

	Scope
	Representative concealed joint compound and backing from 20 interior wall-system locations


Summary by building zone
	Zone
	Wall systems sampled
	Systems with ACM
	Observed asbestos content

	North administration
	7
	7
	3–7% chrysotile in joint compound / backing

	Secure briefing core
	4
	4
	4–8% chrysotile in joint compound / backing

	East office corridor
	4
	4
	3–6% chrysotile in joint compound / backing

	West service wing
	5
	4
	2–7% chrysotile in four systems; one negative

	TOTAL
	20
	19
	19 of 20 representative wall systems positive


Laboratory conclusion
Nineteen of the twenty representative wall systems contain asbestos-bearing concealed finish or backing material. On the sampled record, asbestos-containing material is present in approximately ninety-five percent of Campbell Hall's interior wall-system types and is not limited to the utility chases identified in the historical record.
	WORK RESTRICTION. Do not cut, drill, sand, demolish, or remove affected wall assemblies until an approved abatement method, regulated work area, clearance plan, and qualified personnel are in place.


/s/ PARA-MEDIC
Dr. Para-Medic, CIH | Laboratory Technical Director
9 July 2027
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